RUBBER TABLE MAT

Double layer rubber table mat with excellent grounding properties, available in different colors and in complete rolls or pre-cut.

Physical properties :

Elongation : 188%

elastic resilience : 14%

tearing strength: 20.6KN/m

Tensile strength: 3.6Mpa

Thickness : 2.0mm,

Heat resistance:  No soldering resistance

Electrical properties :

Resistant to ground : <3.5x10e7Ω

Surface resistance : <1.0x10e10Ω

Compliant to : IEC 61340-5-1 ; ANSI/ESD S20.20

- Features & part-numbers (Partial Products)

| Shape | Dimension (W x L x T) | Color |
| --- | --- | --- |
| Complete Roll (Shinning) | 0.6m x 10m x 2mm | Green/black |
|  | 0.9m x 10m x 2mm | Green/black |
|  | 1.0m x 10m x 2mm | Green/black |
|  | 1.2m x 10m x 2mm | Green/black |

Options :

Color: Blue, Green, Grey, Brown, Black available

Other cut sizes, roll size ,color, other mat equipments are available.